#### Laying techniques

#### Recommendations in the installation of ceramic products

Adhesion, understood as the strength of the bond between the ceramic piece and the base, plays a vital role in the quality of the tiled surface. Good adhesion should guarantee that the tile is firmly fixed to the base. The development of new low porosity ceramic materials that are resistant to abrasion and sub-zero temperatures, large formats, and their installation in industrial or large commercial areas, facades, etc., has led to a corresponding development in adhesive products.

Increased knowledge about the use of special adhesives means that thick layer installation (mechanical adhesion) is being replaced by thin layer installation (chemical adhesion); the latter offers clear advantages, particularly in relation to quality of both adhesion and durability. The appropriate adhesive must be chosen, taking into account the surface to be tiled and the type of ceramic tile.

It is very important to use the right tools when laying the tiles (notched trowel, white rubber mallet, spirit level and suction cup). The substrate on which the tiles are to be laid must also be free of any plaster, paint residues etc., thus enabling the adhesive to be effective over time.

###### The adhesive manufacturer’s instructions must be followed at all times

#### Movement joints, whether structural, perimeter, dilation or laying joints, must always be respected for a perfect installation.

##### Structural joints:

These must always follow the instructions given in the project by a specialised engineer or architect.

##### Perimeter joints:

These must be continuous and no less than 8 mm wide. Their purpose is to insulate the ceramic floor tiles from other tiled surfaces such as walls (hidden by the skirting), columns or doors.

###### The omission of perimeter joints is one of the most frequent causes of ceramic tile lifting.

##### Partition joints:

Partition or expansion joints are used to allow for deformations caused by the temperature variations between the tile, the adhesive and the substrate. Large tiled surface areas must be subdivided into smaller sections, delimited by partition joints, in order to avoid stress caused by expansion and contraction. Where floors are subject to high pedestrian traffic, hard wheels or the dragging of heavy loads, specially designed partition joints suitable for heavy loads must be used.

##### Installation joints:

To protect against any structural (expansion- contraction) movements, a separation joint must be fitted between all contiguous tiles.

These should be laid with a separation of no less than 2-3 mm. Installation joints offer several advantages: they help to absorb deformations caused by the substrate and ameliorate the stress generated on the bottom of the tile when the floor is subject to loads. Accumulated stress may eventually cause tiles to lift. They also have an important aesthetic function and highlight the beauty of the tile. The joints can have a smooth finish, level with the tiles, or a sunken concave finish. They are generally applied to interior and exterior tiled walls.

Low porosity, deformable and water-resistant grouts are also available. Suitable for facades, floors subject to heavy and local traffic with persistent presence of water. For surfaces where the presence of acids and alkalis is commonplace, such as food or health related premises, two-component reactive resins such as epoxy grouts should be used. This type of grouting material is composed of synthetic resins (usually epoxy resin). Their main properties are: resistance to chemicals, bacterial resistance, very good resistance to damp and excellent resistance to abrasion.

###### The adhesive manufacturer’s instructions must be followed at all times

##### The minimum separation between tiles should be no less than 2-3 mm for interiors and 3-5 mm for outside areas.

Classification of grouts according to the EN 13888 standard

##### MODIFIED CEMENT-BASED GROUTS CG2

Optional ArW (high abrasion resistance and low water absorption)

##### REACTIVE RESIN-BASED GROUTS RG

Generally two-component grouts, epoxy based, resistant to chemicals, completely impermeable and highly resistant to compression.

##### The use of grouts containing micronised carbon (carbon black) should always be avoided

#### Griffstoff

Two techniques are used for laying ceramic tiles: the thick layer and the thin layer methods.

#### It is very important to remember that the installation of porcelain stoneware requires the substrate to be completely level and free of any substances that may interfere with efficient adhesion. The thin layer technique must always be employed, using a notched trowel, a white rubber mallet, a spirit level and a suction cup. For outside applications and formats larger than 900 cm2, the double bonding technique should be used, i.e., the adhesive is applied to both the substrate and the back of the tile.

###### The adhesive manufacturer’s instructions must be followed at all times

##### The thick layer method.

This is the traditional technique for laying tiles, whereby the tile is laid directly onto the substrate (partition wall, brick, reinforced concrete). This is a cheaper me thod and also enables defects in levels to be corrected. The adhesive material used with this method is traditional mortar.

##### The thin layer method, (with adhesives).

This is a more recent technique, adapted for use with modern ceramic materials and a wide range of substrates. The tiles are usually laid on a previously prepared base, whether plastered walls or a cement floor base.

This technique has clear advantages: it is suitable for any type of ceramic tile and is compatible with all substrates. Appropriate adhesives are available for all types of base and ceramic tiles and they offer ample rectification time. They absorb any deformation in the substrate and their adhesive performance is higher. The adhesive materials used with this method are cement-based adhesives, adhesive pastes and reaction resin adhesives. The following types of cement glues may be considered, depending on the properties of the ceramic tile to be laid.

Adhesives are classified according to the EN 12004 and 12002 standards for ceramic tile adhesive and deformability

#### Leveling Systems

##### GLAZED BREAKAGE IN RECTIFIED TILES

When we talk about coatings and installation systems, we must take into account the following considerations:
Materials Absorption group BIII, absorption greater than 10%.
More fragile.
Rectified, they have a micro bevel or minimum bevel
The problem is that the edge of these pieces is very delicate and any small pressure can cause the edge to chip.

#### Traditional system

In these systems, the wedges are in contact with the ceramic, and by exerting pressure, spalling can occur. This is due to the fact that at the moment of tightening the wedge, we generate a pressure causing the divider to be less than 90◦ tilting the divider and exerting pressure on the bevel.

Example of inclined divider exerting pressure on the bevel, leveling system parts, and example of traditional placement.

What solution have the manufacturers of leveling systems found to solve this problem that the entire sector presents?

Leveling system manufacturers have designed modifications for these types of products.

#### Protector leveling systems

The protector is placed under the wedge to achieve a perfect finish of the flooring or tiling, eliminating friction in the force between the wedge, the divider and the ceramic.

Specially designed to protect tiles, especially in the case of delicate and thin ceramics.

##### USE OF THE PROTECTOR

Техники на полагане

Препоръки при монтаж на керамични изделия

Лепилото, което е силата на връзката между керамичния детайл и основата, играе жизненоважна роля за качеството на облицованата повърхност. Доброто лепило трябва да гарантира, че плочката е здраво фиксирана към основата. Разработването на нови керамични материали с ниска порьозност, които са устойчиви на абразия и минусови температури, големи формати и тяхното инсталиране в промишлени или големи търговски площи, фасади и др., доведе до съответното развитие на лепилните продукти.

Повишените познания за използването на специални лепила означават, че монтажът на дебел слой (механично залепване) се заменя с монтаж на тънък слой (химическо залепване); последното предлага ясни предимства, особено по отношение на качеството както на залепянето, така и на издръжливостта. Трябва да се избере подходящото лепило, като се вземе предвид повърхността, която ще се облицова и вида на керамичните плочки.

Много е важно да използвате правилните инструменти, когато полагате плочките (назъбена мистрия, бял гумен чук, нивелир и вендуза). Основата, върху която ще се полагат плочките, също трябва да бъде почистена от мазилка, остатъци от боя и др., което позволява на лепилото да бъде ефективно във времето.

Инструкциите на производителя на лепилото трябва да се спазват през цялото време

Деформационните фуги, независимо дали са конструктивни, периметърни, дилатационни или полагащи фуги, трябва винаги да се спазват за перфектен монтаж.

Конструктивни съединения:

Те винаги трябва да следват инструкциите, дадени в проекта от специализиран инженер или архитект.

Периметрови фуги:

Те трябва да са непрекъснати и с ширина не по-малко от 8 mm. Предназначението им е да изолират подовите керамични плочки от други облицовани повърхности като стени (скрити от первази), колони или врати.

Липсата на периметрови фуги е една от най-честите причини за повдигане на керамичните плочки.

Преградни фуги:

Преградните или дилатационните фуги се използват, за да позволят деформации, причинени от температурните промени между плочката, лепилото и основата. Големите повърхности, облицовани с плочки, трябва да бъдат разделени на по-малки секции, ограничени от преградни фуги, за да се избегне напрежението, причинено от разширяване и свиване. Когато подовете са обект на висок трафик на пешеходци, твърди колела или влачене на тежки товари, трябва да се използват специално проектирани преградни фуги, подходящи за големи натоварвания.

Монтажни фуги:

За да се предпази от каквито и да било структурни (разширяване-свиване) движения, трябва да се постави разделителна фуга между всички съседни плочки.

Те трябва да се полагат с дебелина не по-малко от 2-3 mm. Монтажните фуги предлагат няколко предимства: те помагат за поемане на деформации, причинени от основата, и облекчават напрежението, генерирано в долната част на плочката, когато подът е подложен на натоварване. Натрупаното напрежение в крайна сметка може да доведе до повдигане на плочките. Те имат и важна естетическа функция и подчертават красотата на плочката. Фугите могат да имат гладко покритие, на нивото на плочките или хлътнало вдлъбнато покритие. Обикновено се прилагат за вътрешни и външни стени с плочки.

Предлагат се и нископорьозни, деформируеми и водоустойчиви фугиращи смеси. Подходящи са за фасади, подове, подложени на интензивен и локален трафик с постоянно наличие на вода. За повърхности, където присъствието на киселини и основи е обичайно, като помещения, свързани със хранителна или здравна дейност, трябва да се използват двукомпонентни реактивни смоли като епоксидни фугиращи смеси. Този тип фугиращ материал се състои от синтетични смоли (обикновено епоксидна смола). Основните им свойства са: устойчивост на химикали, устойчивост на бактерии, много добра устойчивост на влага и отлична устойчивост на абразия.

Инструкциите на производителя на лепилото трябва да се спазват през цялото време

Минималното разстояние между плочките трябва да бъде не по-малко от 2-3 мм за вътрешни и 3-5 мм за външни площи.

Класификация на фугиращите смеси съгласно стандарт EN 13888

МОДИФИЦИРАНИ ФУГИРАЩИ СМЕСИ НА ЦИМЕНТОВА ОСНОВА CG2

Допълнителен ArW (висока устойчивост на абразия и ниска водопоглъщаемост)

РЕАКТИВНИ ФУГИРАЩИ СМЕСИ НА БАЗА НА СМОЛА RG

Обикновено двукомпонентни фугиращи смеси на епоксидна основа, устойчиви на химикали, напълно непропускливи и силно устойчиви на компресия.

Винаги трябва да се избягва използването на фугиращи смеси, съдържащи микронизиран въглерод (сажди).

Грифстоф

Използват се две техники за полагане на керамични плочки: дебелослоен и тънкослоен метод.

Много е важно да запомните, че монтажът на гранитогрес изисква основата да бъде напълно равна и без никакви вещества, които могат да попречат на ефективното залепяне. Винаги трябва да се използва техниката на тънък слой, като се използва назъбена маламашка, бял гумен чук, нивелир и вендуза. За външни приложения и формати, по-големи от 900 cm2, трябва да се използва техниката на двойно залепване, т.е. лепилото се нанася както върху основата, така и върху гърба на плочката.

Инструкциите на производителя на лепилото трябва да се спазват през цялото време